SECTION 08620

PLASTIC GLAZED HURRICANE RESISTANT SKYLIGHTS

Curb Mount / Hurricane Resistant

PART 1-GENERAL

  - SUMMARY

- This section includes the following:

  - CWS2 model standard curb mount, double dome, impact resistant.

  - CWS3 model standard curb mount, triple dome, impact resistant.

[Formerly Wasco Models DDCS-HU, DDDCS-HU]

- Related Sections:  The following sections contain requirements that relate to this section:

  - Division Six Section “Rough Carpentry” for wood curbs and nailers.

  - Division Seven Section “Roof Accessories” for curbs, roof hatches, and smoke vents.

  - Division Seven Section “Flashing and Sheet Metal” for metal flashing for skylights.

C.  Refer to roofing system sections for roofing accessories to be built into the roofing system to          accommodate work of this section.

  - PERFORMANCE REQUIREMENTS

- General:  Provide unit skylights capable of withstanding loads as prescribed by the prevailing code for the project location.

- Unit skylights must be tested in accordance with AAMA\WDMA\CSA\101\I.S.2\A440 as required by Section 2405.5 of the International Building Code.

- Units shall be approved and listed by the Florida Building Commission with a current Florida Product Approval number.

- Units shall be tested per Florida Building Code test protocols for High Velocity Hurricane Zones, protocols TAS 201, TAS 202, and TAS 203.

- Units shall be rated for both Large and Small Missile impact.

- Load capabilities of units are size dependent.  Contact factory for assistance.

1.3 SUBMITTALS

- Product Data Sheet:  For each type of skylight specified, include details of construction and installation, relative to applicable roofing materials.

- Samples for Selection:  Manufacturer’s color charts showing a full range of colors available for each type of skylight glazing and Aluminum Finish.

  - QUALITY ASSURANCE

- Fire-Test-Response Characteristics:  Provide Thermoformed domes fabricated from sheets identical to those tested for the following fire-test-response characteristics, per ASTM test method indicated below, by UL or other testing and inspecting agencies acceptable to authorities having jurisdiction.  Identify plastic sheets with appropriate markings of applicable testing and inspecting organization.

  - Self-Ignition Temperature:  651 deg F (343 deg C) or greater when tested per ASTM D 1929 on plastic sheets in the thickness intended for use.

  - Smoke density of 75 or less when tested per ASTM D 2843 on plastic sheets in the thickness intended for use.

  - Relative- Burning Characteristics:  As follows, when tested per ASTM D 635:

    - CC2:  Burning rate of 2.5 inches (64 mm) per minute or less when tested on plastic glazing indicated above with a nominal thickness of 0.060 inch (1.5 mm) or the thickness intended for use.

  - WARRANTY

- General:  Warranties specified in this section shall not deprive the Owner of other rights the Owner may have under other provisions of the Contract Documents and shall be in addition to and run concurrent with other warranties made by the Contractor under requirements of the Contract Documents.

- Skylight Warranty:  Provide written warranty signed by manufacturer, agreeing to repair or replace work that exhibits defects in materials or workmanship and guaranteeing weather-tight and leak-free performance.  “Defects” is defined as uncontrolled leakage of water and abnormal aging or deterioration.

  - Warranty Period:  5 years from date of Substantial Completion.

- Plastic Warranty:  Provide written warranty signed by manufacturer agreeing to repair or replace work that has or develops defects in the plastic.  “Defects” is defined as abnormal aging or deterioration.

  - Warranty Period for Acrylic:  5 years from date of Substantial Completion.

- Finish Warranty:  Provide written warranty signed by manufacturer agreeing to repair or replace work with finish defects.  “Defects” is defined as peeling, chipping, chalking, fading, abnormal aging or deterioration, and failure to perform as required.

- Warranty Period for Anodized Finish:  5 year from date of shipment from the manufacturer.

- Warranty Period for 2604 Powder Finish:  10 years from date of shipment from the manufacturer.

- Warranty Period for 2605 Liquid Finish:  10 years from date of shipment from the manufacturer.    (20 years available if specified).

- Warranty Period for 2605 Powder Finish: 20 years from the date of shipment from the manufacturer.

PART 2- PRODUCTS

  - MANUFACTURERS

- Manufacturers:  Subject to compliance with requirements, provide products by Wasco Skylights part of the Velux Group, Wells, ME (800-388-0293).

- Substitutions:  Manufactures shall not be considered without prior approval in writing no later than ten (10) calendar days prior to bid.  Substitute manufacturers must have been in the custom skylight business for not less than a period of 15 years and must submit to the Architect the following:

  - List of similar projects successfully completed within the last five years.

  - Proof of financial capability.

  - Complete details of proposed skylight.

  - Complete specifications for Architect’s review.

  - Test reports showing units have been tested and passed in accordance with Florida Building Code requirements for HVHZ.

  - MATERIALS

- Curb Frame:  Bright white high-performance PVC with bronze cap stock and minimum effective thickness of 0.060 inch (1.5mm).  Provide integral condensation gutter system with corners fully welded for waterproof quality.

- Retainer Frame:  Extruded aluminum alloy 6063-T5 (min).  ASTM B 221 (ASTM B 221 M) with minimum effective thickness of 0.60 inch (1.5 mm).

- Plastic Sheets:  Monolithic, formable, transparent (colorless and tinted) sheets with good weather and impact resistant.

- Thermal Break:  Fabricate skylight units with thermal chambered PVC.

- Gaskets: Structural glazing tape to form adhesive bond between PVC curb and inner dome, between inner and outer dome, and between outer dome and extruded aluminum retainer. Gaskets form an air and water impenetrable barrier between adjacent surfaces.

- Fasteners:  Same metal as metals being fastened, or nonmagnetic stainless steel or other non-corrosive metal as recommended by manufacturer.

  - PLASTIC SKYLIGHT UNITS

- General:  Factory-assembled, curb-mounted unit consisting of plastic glazing, gasketing, inner frame designed to mount on separate curb, and self-contained flashing.

  - Products:  Provide model CWS3 meeting the requirements of this section.

- Curb:  Minimum 1 ½” wide, 4” minimum height, field built or pre-fabricated (By others).

- Condensation Control:  Fabricate skylight units with integral internal gutters and weeps to collect and dispose of condensation.

- Thermal Break:  Fabricate skylight units with thermal chambered PVC.

- Shape and Size:  As indicated by model number.

- Glazing:  Outer dome thermoformed impact modified acrylic. (Clear or White).

- Glazing:  Inner dome thermoformed impact modified acrylic.  (Clear or white). (EDIT AS REQUIRED)

  - FABRICATION

- Framing Components:  As follows:

1.     Factory fit and assemble components.

  - Fabricate components that, when assembled, will have accurately fitted joints with ends coped or mitered to produce hairline joints free of burrs and distortion.

  - Fabricate components to drain water passing joints and to drain condensation and moisture occurring or migrating within skylight system to the exterior.

  - Fabricate components to accommodate expansion, contraction, and field adjustment, and to provide for minimum clearance and shimming at skylight perimeter.

  - Fabricate components to ensure that glazing is thermally and physically isolated from framing members.

  - Form shapes with sharp profiles, straight and free of defects or deformations, before finishing.

  - Fit and secure joints by heliarc welding.

2.5 ALUMINUM FINISHES FOR GLAZING RETAINER (EDIT AS REQUIRED)

- General:  Comply with NAAMM “Metal Finishes Manual” recommendations for application and designations of finishes.

- Finish designations prefixed by AA conform to the system for designations of aluminum finishes established by the Aluminum Association.

  - Mill Finish:  Manufacturer’s standard mill finish.

  - 2605 Powder: Powder Coat High-Performance Architectural Coating complying with AAMA 2605. Color:______________

  - 2604 Powder: Powder Coat High-Performance Architectural Coating: complying with AAMA 2604. Color:______________

  - 2605 Liquid: Kynar Fluoropolymer Two-Coat System  (70% PVDF) complying with AAMA 2605.  Color:______________ (3coat and 4 coat available)

  - Anodized: [Clear-Anodized Finish, Class I:  AA-C22A41 complying with AAMA 611.] [Color –Anodized Finish Class I:  AA-C22A42/A44 complying with AAMA 611.  Color:______________]

PART 3- EXECUTION

  - EXAMINATION

- Examine substrates and conditions, with installer present, for compliance with requirements for installation tolerances and other conditions affecting skylight performance.

    - Proceed with installation only after unsatisfactory conditions have been corrected.

  - INSTALLATION

- General:  Comply with manufacturer’s written instructions for protecting, handling, and installing skylight components.

- Coordinate with installation of roof deck and other substrates to receive skylight units.

- Coordinate with installation of vapor barriers, roof insulation, roofing, and flashing as required to assure that each element of the work performs properly and that combined elements are waterproof and weather tight.  Anchor units securely to supporting structural substrates, adequate to withstand lateral and thermal stresses as well as inward and outward loading pressures.

- Counter Flashing:  Where counter flashing is required as a component of the skylight, install to provide an adequate waterproof overlap with roofing or roof flashing (as counter flashing).  Seal with thick bead of mastic sealant, except where overlap is indicated to be left open for ventilation.

  - CLEANING AND PROTECTION

- Clean exposed metal and plastic surfaces according to manufacturer’s instructions.  Touch up damaged metal coatings.

- Final cleaning by others.

END OF SECTION