SECTION 07721

PRE-MANUFACTURED SKYLIGHT CURBS

- GENERAL

      - SUMMARY

        - Section Includes:

          - Owner furnished manufactured steel structural (14ga) roof curbs and adapter curbs for installation by Contractor.

          - Manufactured steel non-structural (18ga) roof curbs furnished and installed by Contractor.

          - Insulated Model: CCA3

          - Non-insulated Model: CCA6

- [Formerly Wasco Models WRC3, WRC6]

        - Related Requirements:

          - Section 01640 - General procedures related to Owner furnished products.

          - Section 01645 – Manufacturers, suppliers, and vendor contacts and product names and numbers.

          - Section 05120 - Structural Steel:  Roof opening frames and headers.

          - Section 05210 - Steel Joists:  Joists supporting roof curbs.

          - Section 07500 - Membrane Roofing: Board insulation for roof curbs.

          - Section 07620 - Sheet Metal Flashing and Trim: Sheet metal flashing installed in conjunction with roof penetration curbs.

          - Section 08631 - Metal Framed Skylights.

      - REFERENCES

        - The publications listed below form a part of this specification to the extent referenced. Publications are referenced within the text by the basic designation only.

        - American Welding Society (AWS):  AWS D1.1 - Structural Welding Code.

        - ASTM International (ASTM):

          - ASTM A 463 - Steel Sheet, Aluminum Coated by the Hot-Dip Process.

          - ASTM A 653 - Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process.

          - ASTM A 792 - Steel Sheet, 55% Aluminum-Zinc Alloy-Coated by the Hot-Dip Process.

        - Steel Structures Painting Council (SSPC):

          - SSPC-Paint 20 - Zinc-Rich Coating Type I - Inorganic and Type II- Organic.

      - DEFINITIONS

        - Structural Roof Curb:  Manufactured square or rectangular roof curb, bearing on structural steel joists or headers, designed to support equipment dead load and roof dead and live loads.

        - Non-Structural Roof Curb:

          - Deck Penetrations - 10 Inches by 10 Inches or Less:  Manufactured square or rectangular roof curb, bearing on top of metal roof deck, designed to receive sheet metal flashing skirt, not used for support of equipment.

          - Deck Penetrations - Greater Than 10 Inches by 10 Inches:  Manufactured square or rectangular roof curb bearing on structural steel angle frame, designed to support equipment dead load. Roof dead and live load supported by structural angle frame.

      - QUALITY ASSURANCE

        - Qualifications for Welding Work:  Qualify field welding operators in accordance with AWS Standard Qualification Procedures. Provide certification that field welders have satisfactorily passed AWS qualification tests within previous 12 months.

          - If recertification of welders is required, provide without additional cost to Owner.

      - DELIVERY, STORAGE AND HANDLING

        - Transport, handle, store, and protect products in compliance with the requirements of Section 01600 and manufacturer's recommendations.  Receive Owner Furnished products in compliance with the requirements of Section 01640.

        - Ship curbs to site palletized and banded.

        - Curb Manufacturer shall furnish Curb Schedule to Contractor identifying curb "Type" and roof penetration for which curb is to be used. Curb Schedule shall identify identical curbs as single "Type" (i.e. Type A- skylights). Stack curbs at site to prevent twisting, bending or permanent deformation.

- PRODUCTS

      - MANUFACTURERS (EDIT AS REQUIRED)

        - Structural Roof Curbs:  Owner’s supplier for structural roof curbs and adapter curbs will be as follows

          - Wasco Part of the VELUX Group – 85 Spencer Drive, Unit A, PO Box 559, Wells, ME 04090. Contact 800-388-0293.

        - Non-Structural Roof Curbs:  Subject to compliance with project requirements, provide prefabricated metal roof curbs by:

          - Wasco Part of the VELUX Group – 85 Spencer Drive, Unit A, PO Box 559, Wells, ME 04090. Contact 800-388-0293.

      - MATERIALS

        - Sheet Steel:  One of the following:

          - Galvanized Steel Sheet:  ASTM A 653, SS (Structural Steel) Classification, Grade 33, G60 hot-dip zinc coating.

          - Aluminum-Coated Steel Sheet:  ASTM A 463, SS (Structural Steel) Classification, Grade 33, Type 2, T2 100 aluminum coating.

          - Aluminum Zinc Alloy-Coated Steel Sheet (GAVALUME):  ASTM A 792, AZ55 aluminum zinc alloy coating.

        - Board Insulation:  Specified in Section 07500.

        - Wood Nailers:  CCA Pressure Treated Lumber Type C, "Standard" grade lumber of any species.

        - Zinc-Rich Primer:  SSPC-Paint 20 Type II.

        - Deck Support Clip:  Galvanized steel sheet, gauge as shown.

        - Finish Paint:

          - Primer:  One coat Speedhide Super Tech Dry-Fog Epoxy Ester #6-157 by PPG.

          - Finish:  One coat Speedhide Super Tech Alkyd Dry-Fog Enamel, Eggshell # 6-151 by PPG.]

      - STRUCTURAL ROOF CURBS

        - Fabrication, General:  Coated 14-gauge steel sheet curb sections, corners fully mitered and welded; 2 inch by 4 inch (nominal dimension) pressure treated continuous wood nailers mechanically fastened with corrosion resistant fasteners at 12 inches on center to exterior face of curb. Shop prime welded connections with zinc-rich paint complying with SSPC-Paint 20.

        - Adapter Curbs:  Curbs shall be fully welded and insulated.  Blank off open areas not used for supply and return air to prevent air mixing.  Construct adapter curbs with the minimum height required to achieve proper airflow.  Verify curb type, size, and unit prior to fabrication.

        - Curb Height:  Unless otherwise required by local codes, minimum curb height from top of bar joist to top of curb shall be as specified below but in no case less than 8 inches from top of roof membrane to top of curb.

        - Loads indicated on Drawings.

        - Welding:  AWS D1.1.

        - Skylight Curbs Safety Screen:

          - Internal Support Frame for Safety Screen:  14 gauge, 3/4"x3/4" maximum galvanized steel support angle to interior perimeter walls of curb, recessed from top flange 3/4" minimum.  Internal support frame for safety screen to be welded to curb at 12" on center with minimum 1" welds.

          - Safety Screen:  Shop fabricated 3/16 inch cold rolled galvanized steel rods welded in 6 inch by 6 inch grid pattern. Weld screen to internal support frame at each grid point.  Do not mount safety screen on top of curb nor attached to curb wall.  [When venting skylights are used, allow room at top inside face of curb for smoke vent installation.  ]Internal support frame and screen shall have been tested to withstand impact of 245 pound lead weight, 10-3/4 inch diameter, dropped from height of 3 feet and support concentrated load of 600 pounds after impact.]

        - Shop Painting:  Shop finish interior surfaces of curbs including safety screen and hardware kit of items that will be exposed to the public after installation. Use PPG dry fog coating as specified; color to match Sherwin-Williams [#SW6385 “Dover White"].]

      - NON-STRUCTURAL ROOF CURBS (CONTRACTOR FURNISHED AND INSTALLED)

        - Coated 18-gauge steel sheet curb sections, corners fully mitered and welded; 2 inch by 2 inch (nominal dimension) pressure treated continuous wood nailers mechanically fastened at 12 inches on center to exterior face of curb. Shop prime welded connections with zinc-rich paint complying with SSPC-Paint 20. Profile and dimensions shall be as shown.

          - Web Height:  Comply with local code requirements for minimum curb height, but in no case shall curb height be less than 18 inches for deck penetrations greater than 10 inches by 10 inches and not less than 14 inches for deck penetrations 10 inches by 10 inches or less as measured from top of steel roof deck to top of curb, nor shall curb height be less than 8 inches as measured from top of roof membrane to top of curb.

- EXECUTION

      - INSTALLATION

        - Install curbs in accordance with manufacturer's instructions and as indicated on Drawings. Coordinate installation with roof membrane installation requirements specified under other Sections.

        - Roof Curbs Bearing on Steel Angles, Joists, and Headers:

          - Set units in place and secure base to roof structure by welding to top chord of structural member.

          - Secure metal deck to perimeter of curb as indicated on Drawings.

        - Roof Curbs Bearing on Roof Deck:

          - Set units in place and secure base to steel roof deck by self-tapping screw fasteners spaced at a maximum of 12 inches on center, staggered.

      - INTERFACE WITH OTHER WORK

        - Coordinate project requirements for custom adapting and connecting to roof curbs with manufacturers and suppliers of curb mounted items and equipment.

END OF SECTION